| CООМЕТ PROJECT Final Report |  |  |
| --- | --- | --- |
| 1. Ref No.: 455/RU-a/09 | 2. Subject field: CERTIFIED REFERENCE MATERIALS |  |
| 3. Field of cooperation: COMPARISONS |  |  |
| 4. Working Group: Belarus, Germany, Russia and Ukraine |  |  |
| 5. Subject: Pilot comparisons of certified reference materials for composition of alloyed steel, type 5ХВ2СФ (CRM 918-90Р), Х6ВФ (CRM 1527-84Р) and 31Х19Н9МВБТ (CRM 2251-82) |  |  |
| 6. Progress: The works on pilot comparisons of CRM for composition of alloyed steel, type 5ХВ2СФ (6S3) - CRM 918-90Р, CRM for composition of alloyed steel, type Х6ВФ (35S3) - CRM 1527-84Р and CRM for composition of alloyed steel, type 31Х19Н9МВБТ (36S5) - CRM 2251-82 for the content of silicon and vanadium are completed. Laboratories from Belarus, Germany, Russia and Ukraine took part in experimental works on comparisons. The obtained results confirmed the values of certified characteristics of CRMs under consideration and allowed the evaluation of measurement capabilities of the participants. On the basis of completed works the report was prepared, which was considered and endorsed at the 14th meeting of COOMET TC 1.12 “CRMs”, where it was also decided to recommend to the Project Coordinator to present CRMs, used in the comparison, for the recognition as COOMET CRMs. In compliance with this decision, documentation on 3 CRM types was circulated by e-mail among the Contact Persons of TC 1.12 “CRMs” to agree on the possibility of their recognition as COOMET CRMs. The results of the agreement of documentation on 3 CRM types were considered at the 15th meeting of COOMET TC 1.12 “CRMs” the decision was taken to submit CRMs to the 21st COOMET Committee meeting for their recognition as COOMET CRMs. CRM for composition of alloyed steel, type 5ХВ2СФ (6S3), CRM for composition of alloyed steel, type Х6ВФ (35S3) and CRM for composition of alloyed steel, type 31Х19Н9МВБТ (36S5) were recognized as COOMET CRMs at the 21st COOMET Committee meeting (resolution 19 of the minutes) and registered in the Register of COOMET CRMs under the numbers COOMET CRM 0098-2011-RU, COOMET CRM 0099-2011-RU and COOMET CRM 0100-2011-RU respectively. ARMENIA, AZERBAIJAN, BELARUS, BULGARIA, GEORGIA, KAZAKHSTAN, KYRGYZSTAN, LITHUANIA, MOLDOVA and UKRAINE joined the CRM recognition as COOMET CRMs. CRM are intended for measuring mass fraction of vanadium and silicon in the certification of certified reference materials for composition of steels by comparison method. The area of application is metallurgy. |  |  |
| 7. Coordinator’s name: Elena V. Osintseva, acting head of CRM State Service Laboratory, FGUP “The Ural Research Institute for Metrology” (FGUP “UNIIM”) Address: 4, Krasnoarmeyskaya Str., Yekaterinburg, 620000, Russian Federation Теl.: (343) 350 60 68 Fax: (343) 350 24 68 E-mail: ev_osinceva@mail.ru E-mail : intermetron@uniim.ru |  |  |
| 8. Completion date: June 2011 |  |  |
| 9. Coordinator’s signature: |  | 10. Date: 25 June 2011 |