| CООМЕТ PROJECT Final Report |  |  |
| --- | --- | --- |
| 1. Ref No.: 475/RU-a/09 | 2. Subject field: CERTIFIED REFERENCE MATERIALS |  |
| 3. Field of cooperation: COMPARISONS |  |  |
| 4. Working Group: Belarus, Kyrgyzstan, Russia, Ukraine |  |  |
| 5. Subject: Conducting of international comparison tests of CRMs for composition of graphite powder SOG -21 (a set of 5 CRM types). |  |  |
| 6. Progress: The works on comparison tests of 2 CRM types from SOG -21 set for composition of graphite powder for 21elements are completed. Laboratories from Belarus, Kyrgyzstan, Russia and Ukraine took part in experimental works on comparisons. The outcome of international comparisons revealed good agreement of measurement results and confirmation of metrological characteristics of CRMs from SOG -21 set for composition of graphite powder, which was the ground for recommending SOG -21 set as a whole for the recognition as COOMET CRMs. All participating laboratories demonstrated fairly high measurement capabilities, which made it possible to extend the scope of accreditation of analytical testing centres and the use of measurement procedures. The progress of works and the obtained results were preliminary considered at the 15th meeting of TC 1.12 “CRMs”. The scope of works and methods of evaluation of the obtained results are laid down in the report, which, together with documentation on SOG -21 set for composition of graphite powder, was circulated among the Contact Persons of TC 1.12 “CRMs” to agree on the possibility of inclusion of SOG -21 set in the List of CRMs, recommended for the recognition as COOMET CRMs at the 21st COOMET Committee meeting. SOG -21 set for composition of graphite was recognized as COOMET CRMs at the 21st COOMET Committee meeting (resolution 19 of the minutes) and registered in the Register of COOMET CRMs under the number COOMET CRM 0102-2011-RU. ARMENIA, AZERBAIJAN, BELARUS, BULGARIA, KAZAKHSTAN, LITHUANIA, MOLDOVA and UKRAINE joined the recognition of SOG -21 set as COOMET CRMs. SOG -21 is intended for measuring mass fraction of elements in the certification of certified reference materials for composition, metrological certification of measurement procedures, calibration of measurement instruments for spectral analysis of graphite powder of extra high purity (GOST 23463-79). The area of application is metallurgy, chemical industry, atomic power, scientific research. |  |  |
| 7. Coordinator’s name: Dmitry G. Lisienko, The Ural State Technical University, named after the first President of Russia B.N. Eltsyn Address: 19, Mira Str., Yekaterinburg, 620002, Russia Telephone: (343) 375-44-36 Fax: (343) 375-45-05 E-mail: lisienko@dpt.ustu.ru, rektorat@mail.ustu.ru |  |  |
| 8. Completion date: June 2011 |  |  |
| 9. Coordinator’s signature: |  | 10. Date: 25June 2011 |